Process Protocol <device xyz>

Subtitle

| Protocol No.: | Wafer | Okmetic | 771/40393 | Qty. | 50 | prime | 100 mm ,100> |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Substrate: 390 (m n/P 3-5 Ohmcm Surfaces: polished/polished |

| Nr. Process step | Substep | Parameter | Value | Comment Date/signature |
| --- | --- | --- | --- | --- |
| 1.0 Initial cleaning | H2SO4/H2O2 | Temperature [(C]: Time [min]: | 120 7 |  |
|  | DI-water rinse |  |  |  |
|  | Rinser Dryer | 99 s /111 s / 222 s |  |  |
| 2. Oxidation | Oxidation Wet 500 nm ( 2 nm | Process name: Process temperature [(C]: Process time [(C]: Tube no.: batch no.: wafer separation during ox.: | FOX1000 1000 1h 26 m 1B4 |  |
|  | Measurement Film thickness | n (Ellipsometer): Program (MPV): | 45 |  |
|  |  | Left | Center left | Center right | right |
|  |  | W.No. L: | W.No. C: | W.No. R: | W.No. L: | W.No. C: | W.No. R: | W.No. L: | W.No. C: | W.No. R: | W.No. L: | W.No. C: | W.No. R: |
|  | d [nm] ( [nm] |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Min: Max: |  |  |  |  |  |  |  |  |  |  |  |  |
| 3.0 Lithography | Spin on resist | Resist: Process name: Rpm 1[min-1]: Time [s]: Rpm 2[min-1]: Time[s]: | AZ 1514 |  |
|  | Pre-bake | Temperature [C]: Time [min]: |  |  |
|  | Exposure MA1006 Mask: SiC-Struct. Alignment Mark: 1 | Program: Exposure time [s]: Power (405 nm) [W]: [mW/cm2]: | 3 8 250 20 |  |
|  | Develop | Manually, developer bath Developer: Time [min]: | AZ 1 m 30s |  |
|  | Inspection | Structure width mask: (e.g. alignment mark) Structure width resist: (delta> 0.3 (m -> new Lithography) | 10 (m |  |
| 4.0 Pattern oxide | RIE Oxide etch (Vacutec) | Process name: Process time: SF6 flow [sccm]: Pressure [mbar]: Power [W]: | Nitride etch 4 m 20 150 150 |  |
|  | Inspection: | Etch rate oxide: |  |  |